| Test date | 24.04.2024 |
| --- | --- |
| Operator | T. Märtson |
| Test method | EVS-EN ISO 4136:2012 |
| Method name | Destructive tests on welds in metallic materials - Transverse tensile test |
| Test machine | Instron 8516 |
| Load cell | Load cell +-300 kN |
| Dimensions measuring device | Caliper TESA nr.7H 1261 01 |
| Sample description | Flat dogbone sample |
| Notes | - |

Test results

|  | Specimen identification | Fm (kN) | Rm (MPa) | Thickness (mm) | Width (mm) | Location of fracture | Remark |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | TT | 129 | 642 | 8 | 25,2 | Weld | - |

Photo of tested specimens