| Date of testing: |  | 24.04.24 |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Test operator: |  | T. Märtson |  |  |  |  |  |
| Test method: |  | Bend test (EN ISO 5173:2023) with former |  |  |  |  |  |
| Temperature: |  | +21 °C |  |  |  |  |  |
| Notes: |  | - |  |  |  |  |  |
| Bend test results |  |  |  |  |  |  |  |
| Test piece |  |  |  | Former diameter, mm | Distance between rollers, mm | Bend angle, ° | Remark |
| Identification of test specimens |  | Dimensions, mm |  |  |  |  |  |
|  |  | Thickness, mm | Width, mm |  |  |  |  |
| SB-1 |  | 10 | 10 | 75 | 95 | 180 | No crack |
| SB-2 |  | 10 | 10 | 75 | 95 | 180 | No crack |
| SB-3 |  | 10 | 10 | 75 | 95 | 180 | No crack |
| SB-4 |  | 10 | 10 | 75 | 95 | 180 | No crack |

Photo of tested specimens