| Date of testing: |  | 01.02.24 |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Test operator: |  | T. Märtson |  |  |  |  |  |
| Test method: |  | Bend test (EN ISO 5173:2023) with former |  |  |  |  |  |
| Temperature: |  | +21 °C |  |  |  |  |  |
| Notes: |  | - |  |  |  |  |  |
| Bend test results |  |  |  |  |  |  |  |
| Test piece |  |  |  | Former diameter, mm | Distance between rollers, mm | Bend angle, ° | Remark |
| Identification of test specimens |  | Dimensions, mm |  |  |  |  |  |
|  |  | Thickness, mm | Width, mm |  |  |  |  |
| FB-1 |  | 4 | 16 | 16 | 28 | 180 | No crack |
| FB-2 |  | 4 | 16 | 16 | 28 | 180 | No crack |
| RB-1 |  | 4 | 16 | 16 | 28 | 180 | No crack |
| RB-2 |  | 4 | 16 | 16 | 28 | 180 | No crack |

Photo of tested specimens