| Test date | 25.06.2024 |
| --- | --- |
| Operator | T. Märtson |
| Test method | EVS-EN ISO 4136:2012 |
| Method name | Destructive tests on welds in metallic materials - Transverse tensile test |
| Test machine | WPM 30t |
| Load cell | Load cell +-300 kN |
| Dimensions measuring device | Caliper TESA nr.7H 1261 01 |
| Sample description | Flat dogbone sample |
| Notes | - |

Test results

|  | Specimen identification | Fm (kN) | Rm (MPa) | Thicknes | WIdth | Section area (mm2) | Location of fracture |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | TT | 119 | 467 | 10,15 | 25,1 | 254,765 | Parent metal |

Photo of tested specimens