| Test date | 27.06.2024 |
| --- | --- |
| Operator | T. Märtson |
| Test method | EVS-EN ISO 4136:2012 |
| Method name | Destructive tests on welds in metallic materials - Transverse tensile test |
| Test machine | Instron 8516 |
| Load cell | Load cell +-100 kN |
| Dimensions measuring device | Caliper TESA nr.7H 1261 01 |
| Sample description | Flat dogbone sample |
| Notes | - |

Test results

|  | Specimen identification | Fm (kN) | Rm (MPa) | Thickness | Width | Section area (mm2) | Location of fracture |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | TT-1 | 10,6 | 541 | 2,0 | 9,8 | 19,6 | HAZ |
| 2 | TT-2 | 10,0 | 505 | 2,0 | 9,9 | 19,8 | HAZ |

Photo of tested specimens